STUDIES ON THE SOLID STATE COPOLYMERIZATION OF POLY (ETHYLENE TEREPHTHALATE) AND POLYCARBONATE OLIGOMERS

E. Bhoje Gowd and C. Ramesh

## Division of Polymer Chemistry

## National Chemical Laboratory

# Dr. Homi Bhabha Road

Pune, 411 008 India

#### Abstract

Blends of Poly(ethylene terephthalate) (PET) and Polycarbonate (PC) oligomers of varying compositions were made by melt blending. The copolymer, poly(ethylene terephthalate-co-bisphenol A carbonate) was synthesized by simultaneous solid state polymerization and ester-carbonate interchange reaction between the oligomers  of PET and PC in the blend. The reaction was carried out under reduced pressure at temperatures below the melting temperature of the blend samples. DSC and WAXS techniques characterized the structure and morphology of the blends, while 1NMR spectroscopy was used to monitor the progress of interchange reactions between the oligomers. The studies have indicated the amorphisation of the PET and PC crystalline phases in solid state with the progress of solid-state polymerization and interchange reaction.